|  | Ref. nr.: | 30501-7/2015-3 |
| --- | --- | --- |
|  | Code: | 278.2.5 |
|  | Date: | 10.11.2016 |

SUBJECT:

Special technical conditions for qualitative acceptance, delivery and impregnation of beech-wood sleepers/bearers and oak-wood bearers and bridge sleepers

In line with its specific characteristics, SŽ-Infrastruktura d.o.o. maintains special conditions of acceptance which deviate from the conditions stated in EN 13145 and EN 13991 on delivery and impregnation of wood rail sleepers/bearers.

List of the requirements:

GENERAL REQUIREMENTS:

-  Wood sleepers/bearers shall be machine-cut and have sharp edges. They shall be cut on the conveyor belt to length which will produce uniform length across all sleepers/bearers as well as rectangular cross sections of the ends. Wanes are permitted on the upper face of the sleeper/bearer (chairing area), but only in the dimensions listed in the special technical conditions of SŽ-Infrastruktura d.o.o. The bottom face of the sleeper/bearer shall always be sharp-edged. The amount of sleepers/bearers with wanes on the upper face shall not exceed 50% of the order amount.

-  Sleeper/bearer ends shall always be strengthened against splitting with perforated toothed plates or bands (S-hooks alone are insufficient) and, if necessary, they shall be additionally secured with steel straps (so-called »bandages«). The toothed plates or bands shall be machine-fit to ensure equal pressing force.

-  Every sleeper shall always have the chairing area planed into a flat surface, shall have diffuse holes drilled on the bottom face, and shall have a numerator nail with imprinted year of production and impregnation fastened on the upper face about 15cm from the edge of the sleeper end.

-  The weight of unimpregnated sleepers/bearers can range from 650kg/m3 to max 830 kg/m3 for oak sleepers/bearers and from 650kg/m3 to max 900 kg/m3 for beech sleepers/bearers (the moisture content air-dried wood shall be between 22% and 30%).

-  The sleepers/bearers shall be impregnated by creosote oil  WEI-type C, manufactured according to European specifications on creosote; the impregnation shall be based on simple Rüpping method (oak timber) and double Rüpping method (beech timber).

-  During the qualitative acceptance procedure, the sleepers/bearers shall be accepted in unimpregnated and suitably dry condition unit-by-unit, with each sleeper turned over and examined from all sides. The sleepers are marked with the marking tool by the consignee.

- The supplier is obliged to fasten a steel strap on any sleepers/bearers which had been deformed during the impregnation (curves, fissures) if the deformation is within the persmissible norms,  or replace them with suitable new units.

If over 20% of sleepers/bearers are rejected, the consignee can choose to discontinue the qualitative acceptance procedure.

DEVIATIONS FROM EN 13145:

5.1.1. Sleepers   -    Picture 7

Form E1 -  d=min 20cm    r=min 12cm

Form E2 -  d=min 21cm    r=min 12cm

5.1.2 Bearers   -   Picture 8

Wanes are permitted on the upper face only and can have the following dimensions:

-  Double-sided: 3cm in width from the upper edge at both sides and 4cm in height.  ( d=20 cm, r =12 cm)

-  Single-sided: 5cm in width from the upper edge and 4cm in height.     (d1=21 cm, r =12 cm)

Oak bridge sleepers:

-  Double-sided: 3cm in width from the upper edge at both sides and 4cm in height.

-  Single-sided: 5cm in width from the upper edge and 4cm in height.

5.3. Tolerances  -   Sleeper/Bearer length: + 1cm/ - 0cm

6.2. Untreated sleepers and bearers

Table 2 :

Sapwood – Permitted in oak bearers and bridge sleepers, when completely sound, but not permitted in the chairing area. It is also not permitted to ever exceed the following dimensions:

- Single-sided: 5cm in width from the upper edge and 4cm in height.

- Double-sided 3cm in width from the upper edge and 4cm in height.

Sapwood not permitted on bottom edge or face of the sleeper/bearer.

Table 2 :

Picture 9 – Maximum accepted dimensions for red beech heart

7cm

10cm

The maximum dimension of red heart in quarter-sawn sleepers/bearers is 10cm in width and 7cm in height.

Table 2 :

Splits – Maximum split length at the ends shall be 250mm, maximum split width shall be 3mm, obligatory anti-splitting protection at the ends by means of perforated toothed plates and additional protection by means of steel straps – bandages.

Table 2 :

Check (upper face) – Maximum length 70cm, maximum width 3mm, and maximum depth 2cm.

Table 2 :

Heart shake (bottom face) – Shake heigth is not permitted to exceed 1/4 of total sleeper/bearer height (4cm). Maximum width of the heart shake is 1cm and maximum length 100cm. A single sleeper/bearer is permitted to have a maximum of two heart shakes. The shake is not permitted to extend over the entire length of the sleeper/bearer.

Table 2 :

Ring shake) – Not permitted

Table 2:

Spring – Maximum 0.4% for sleepers and bearers.

Bow (downward) – Maximum 0.4% for sleepers and bearers.

Bow (upward) – Not permitted

- The technical requirements may be further adjusted according to the specific characteristics of the product.

- The special technical conditions are a mandatory annex to the tender dossier and the contracts concluded for the supply of impregnated sleepers/bearers. .

| Prepared by: |  |  |
| --- | --- | --- |
| Boris Čerle |  | Matjaž Kranjc |
|  |  | Director |
|  |  | Facsimile signature |

Annex:

- Special technical conditions for qualitative acceptance and impregnation of sleepers